Quarterly Report – Public Page

Date of Report: 6th Quarterly Report, June 30, 2025

Contract Number:  693JK32310010POTA

Prepared for: Government Agency: DOT and Co-funders

Project Title: Standardize the Application of Vapor Corrosion Inhibitors

Prepared by: Pipeline Research Council International (PRCI), Inc.

Contact Information:  Janie Norton, jnorton@prci.org 703-205-1600 ext: 105

For quarterly period ending:  June 30, 2025

1: Items Completed During this Quarterly Period:

| Item # | Task # | Activity/Deliverable | Title | Federal Cost | Cost Share |
| --- | --- | --- | --- | --- | --- |
| 17 | 3 | Analyze corrosion probe data from the VCI effect experiments | Results to be included in the quarterly report | $3,127 | $782 |
| 18 | 5 | 7th quarterly status report & project management | Submit 7th quarterly report | $7,448 | $1,862 |

2: Items Not Completed During this Quarterly Period:

None.

3: Project Financial Tracking During this Quarterly Period:

Note that this chart reflects Federal share only:

4:  Project Technical Status –

Item 17, Task 3  Analyze corrosion probe data from the VCI effect experiments. Results to be included in the quarterly report:  The ER probes are being used in several tests in the VCI-effect test matrix.  The various tests parameters and ER probe derived corrosion rates are listed in Table 1; it is noted that the ER probe derived corrosion rates are for 42-day duration.

| Table 1. Test Parameters and ER Probe Derived Corrosion Rates in the VCI Effect Experiments |  |  |  |  |
| --- | --- | --- | --- | --- |
| Test Parameter |  |  |  | ER Probe Corrosion rate (mpy) |
| Chloride (ppm) | Nitrate (ppm) | Moisture (%) | VCI |  |
| 38 | 4 | 75 | VCI-A | 0.3 |
| 244 | 23 | 75 |  | 0.01 |
| 64 | 16 | 75 |  | 3.5 |
| 0 | 423 | 75 |  | 1.4 |
| 38 | 4 | 75 | VCI-B | 0.4 |
| 244 | 23 | 75 |  | 1.1 |
| 64 | 16 | 75 |  | 1.3 |
| 0 | 423 | 75 |  | 0.7 |

The monitoring data indicate that VCIs are able to effectively mitigate corrosion in all but one condition; it is not clear why ER probe corrosion rates are as high as 3.5 mpy in the 65 ppm chloride and VCI-A.

This activity links to item 8 in Attachment 1 Team Project Activities.  This activity links to item 10 in Attachment 2 Project Deliverables.

Item 18, Task 5  7th quarterly status report & project management. Submit 7th quarterly report:  The sixth quarter meeting was held on June 12, 2025.  This report satisfies this item.  This activity links to items 11 and 13 in Attachment 1 Team Project Activities.  This activity links to item 13 in Attachment 2 Project Deliverables.

5: Project Schedule –

The project is on schedule.